BRITISH STANDARD

BS EN ISO

3385:1995

Incorporating

Amendment No. 1

Flexible cellular

polymeric materials —

Determination of

fatigue by

constant-load pounding

The European Standard EN ISO 3385:1995 has the status of a

national standard

BS EN ISO 3385:1995

Committees responsible for this

British Standard

The preparation of this British Standard was entrusted to Technical

Committee PRI/24, Testing of rigid and flexible cellular materials, upon which

the following bodies were represented:

British Plastics Federation

British Railways Board

British Rigid Urethane Foam Manufacturers’ Association

British Rubber Manufacturers’ Association Ltd.

Department of the Environment (Building Research Establishment)

Furniture Industry Research Association

Furniture, Timber and Allied Trades Union

Ministry of Defence

National Bed Federation Limited

Phenolic Foam Manufacturers’ Association

RAPRA Technology Ltd.

Society of British Aerospace Companies Limited

Society of Motor Manufacturers and Traders Limited

This British Standard, having

been prepared under the

direction of the Sector Board for

Materials and Chemicals Sector

Board, was published under the

authority of the Standards

Board and comes into effect on

15 July 1995

© BSI 05-1999

The following BSI references

relate to the work on this

standard:

Committee reference PRI/24

Draft for comment 94/300611 DC

ISBN 0 580 23735 4

Amendments issued since publication

Amd. No.

8970

Date

December

1995

Comments

Indicated by a sideline in the margin

BS EN ISO 3385:1995

Contents

Page

Committees responsibleInside front cover

National forewordii

Foreword2

1Scope3

2Normative reference3

3Principle3

4Apparatus3

5Test pieces3

6Procedure4

7Expression of results4

8Test report4

Figure 1 — Diagrammatic arrangement for manually adjusted machine5

Figure 2 — Diagrammatic arrangement for automatically

adjusted machine6

List of referencesInside back cover

© BSI 05-1999

i

BS EN ISO 3385:1995

National foreword

This British Standard has been prepared by Technical Committee PRI/24 and is

the English language version of EN ISO 3385:1995 Flexible cellular polymeric

materials — Determination of fatigue by constant-load pounding, published by

the European Committee for Standardization (CEN). It is identical with

ISO 3385:1989, published by the International Organization for

Standardization (ISO). It supersedes BS 4443-5:1980, which is withdrawn.

Cross-reference

Publication referred to

Corresponding British Standard

ISO 2439:1980

Polymeric materials, cellular flexible — Determination

of hardness (indentation technique)

A British Standard does not purport to include all the necessary provisions of a

contract. Users of British Standards are responsible for their correct application.

Compliance with a British Standard does not of itself confer immunity

from legal obligations.

Summary of pages

This document comprises a front cover, an inside front cover, pages i and ii,

the EN ISO title page, pages 2 to 6, an inside back cover and a back cover.

This standard has been updated (see copyright date) and may have had

amendments incorporated. This will be indicated in the amendment table on

the inside front cover.

ii

© BSI 05-1999

EUROPEAN STANDARD

NORME EUROPÉENNE

EUROPÄISCHE NORM

ICS 83.100

EN ISO 3385

May 1995

Descriptors: Cellular materials, flexible cellular materials, tests, compression test, fatigue

English version

Flexible cellular polymeric materials —

Determination of fatigue by constant-load pounding

(ISO 3385:1989)

Matériaux polyméres alvéolaires souples —

Détermination de la fatigue par indentation à

charge constante

(ISO 3385:1989)

Polymere Weichschaumstoffe — Bestimmung

der Ermüdung durch konstante Stoßbelastung

(ISO 3385:1989)

This European Standard was approved by CEN on 1995-05-11. CEN members

are bound to comply with the CEN/CENELEC Internal Regulations which

stipulate the conditions for giving this European Standard the status of a

national standard without any alteration.

Up-to-date lists and bibliographical references concerning such national

standards may be obtained on application to the Central Secretariat or to any

CEN member.

This European Standard exists in three official versions (English, French,

German). A version in any other language made by translation under the

responsibility of a CEN member into its own language and notified to the

Central Secretariat has the same status as the official versions.

CEN members are the national standards bodies of Austria, Belgium,

Denmark, Finland, France, Germany, Greece, Iceland, Ireland, Italy,

Luxembourg, Netherlands, Norway, Portugal, Spain, Sweden, Switzerland and

United Kingdom.

CEN

European Committee for Standardization

Comité Européen de Normalisation

Europäisches Komitee für Normung

Central Secretariat: rue de Stassart 36, B-1050 Brussels

© 1995 Copyright reserved to all CEN members

Ref. No. EN ISO 3385:1995 E

EN ISO 3385:1995

Foreword

The text of the international standard from

ISO/TC 45, Rubber and rubber products, of the

International Organization for Standardization

(ISO) has been taken over as a European Standard

by the Technical Committee CEN/TC 249, Plastics.

This European Standard shall be given the status of

a national standard, either by publication of an

identical text or by endorsement, at the latest by

November 1995, and conflicting national standards

shall be withdrawn at the latest by November 1995.

According to CEN/CENELEC Internal Regulations,

the following countries are bound to implement this

European Standard: Austria, Belgium, Denmark,

Finland, France, Germany, Greece, Iceland,

Ireland, Italy, Luxembourg, Netherlands, Norway,

Portugal, Spain, Sweden, Switzerland and United

Kingdom.

2

© BSI 05-1999

EN ISO 3385:1995

1 Scope

This International Standard specifies a method for

the determination of loss in thickness and loss in

hardness of flexible cellular materials intended for

use in upholstery.

This test method provides a means of assessing the

service performance of flexible cellular materials of

the latex and polyether urethane types used in

load-bearing upholstery.

The measured loss in thickness and loss in hardness

are related to, but are not necessarily the same as,

the losses likely to occur in service.

The method is applicable both to standard size test

pieces cut from stock material and to shaped

components.

2 Normative reference

The following standard contains provisions which,

through reference in this text, constitute provisions

of this International Standard. At the time of

publication, the edition indicated was valid. All

standards are subject to revision, and parties to

agreements based on this International Standard

are encouraged to investigate the possibility of

applying the most recent edition of the standard

indicated below. Members of IEC and ISO maintain

registers of currently valid International Standards.

ISO 2439:1980, Polymeric materials, cellular

flexible — Determination of hardness

(indentation technique).

By means of a crank or other suitable mechanism,

the machine shall be capable of oscillating either the

platen (4.1) carrying the test piece, or the indentor

support mounting (4.3), towards the other in a

vertical direction at a rate of (70 ± 5) strokes per

minute. The amplitude of the stroke shall be

adjustable.

4.3 Indentor support mounting, such that the

indentor force is carried by it except at that part of

the stroke when the mounting and platen are closest

together; at this point the full force of the indentor

shall be supported by the test piece. The indentor

shall be free to be lifted in its mounting to prevent

overloading of the test piece. Means shall be

provided whereby at any stroke the time can be

controlled during which the full force is exerted by

the indentor. This time shall be no more than 25 %

of the total duration of each cycle.

4.4 Force measuring device, whereby the load

applied to the test piece by the indentor can be

measured. A suitable method consists in mounting

the platen upon load cells.

NOTE Where adjustment is manual, the indentor is attached to

the lower end of a shaft which passes through a vertical guide

above the platen carrying the test piece. Adjustment of the

vertical position of the indentor relative to the platen controls the

length of time at any stroke that the full force of the indentor is

supported by the test piece. A suggested arrangement is shown

diagrammatically in Figure 1.

A suggested method of securing automatic adjustment is shown

in Figure 2, whereby the length of time during which the test

piece supports the indentor is controlled directly by the time

during which the valve is open.

3 Principle

Repeated indentation of a test piece by an indentor

smaller in area than the test piece, the maximum

load reached during each cycle being kept within

specified limits.

5 Test pieces

5.1 Shape and dimensions

Test pieces shall be right parallelepipeds having

sides of length 380 mm ± 20 mm and a thickness

of 50 mm ± 2 mm. Tests may also be carried out on

components that do not comply with these

dimensions subject to agreement between the

interested parties.

5.2 Samples showing orientation

If the products show an orientation of the cellular

structure, the direction in which the indentation is

to be carried out shall be agreed upon between the

interested parties. Normally, testing is carried out

in that direction in which the finished product will

be stressed under service conditions.

5.3 Number

Three test pieces shall be tested.

4 Apparatus

Pounding test machine, having the following parts.

4.1 Plane platen, capable of fully supporting the test

piece, and suitably vented with holes

approximately 6 mm in diameter at

approximately 20 mm pitch in order to allow air to

escape from the test piece.

4.2 Indentor, having an overall diameter

of 250 mm ± 1 mm with a 25 mm ± 1 mm radius at

its lower edge, provided with a device for applying a

maximum force of 750 N ± 20 N during one loading

cycle. The indentor shall be rigidly fixed to its guide

and its surface shall be smooth but not polished.

© BSI 05-1999

3

EN ISO 3385:1995

5.4 Conditioning

Test pieces shall not be tested less than 72 h after

manufacture unless it can be demonstrated that, at

either 16 h or 48 h after manufacture, the

compression stress-strain characteristics obtained

do not differ by more than ± 10 % from those

obtained after 72 h. Testing is permitted at

either 16 h or 48 h if, at the selected time, the above

criterion has been satisfied.

Prior to the test, the test pieces shall be stored for at

least 16 h at either

23 °C ± 2 °C, 50 % ± 5 % relative humidity, or

27 °C ± 2 °C, 65 % ± 5 % relative humidity.

This period can form the latter part of the period

following manufacture.

7 Expression of results

7.1 Loss in thickness

The percentage loss in thickness %d given by the

formula

d1 – d2

%d = 100 ×--------------------

d1

where

d1 is the original thickness;

d2 is the final thickness.

Express the result as the median of the values

obtained for the three test pieces.

7.2 Loss in hardness

The loss in hardness %H is given by the formula

%H = H1 – H2

where

H1 is the original hardness;

H2 is the final hardness.

Express the result as the median of the values

obtained for the three test pieces.

NOTE This method of expressing hardness loss results as

absolute rather than percentage losses has been selected because

analysis of experimental data shows that the variability of

results is reduced by this method of expression. The commonly

used percentage loss is related to the absolute loss by the

following formula:

H1 – H 2

-Percentage hardness loss = 100 ×-------------------

H1

6 Procedure

Measure the thickness d1 of one of the test pieces

and its hardness index as specified in ISO 2439.

Place the test piece concentrically under the

indentor, adjust the stroke to be equal to the

thickness of the test piece and adjust the relative

positions of the indentor and platen until the

specified load of 750 N ± 20 N is applied.

Adjustment of the indentor mass may be required.

NOTE In the case of the manually adjusted arrangement

shown in Figure 1, the correct setting is achieved when the

indentor is just lifted in its mounting. In the case of the

arrangement shown in Figure 2, these adjustments are

automatic. However, slight movement of the indentor in its

mounting may not be clearly visible, but provided that the valve

is operated at each stroke, the conditions of the test are satisfied.

As the foam softens during the test, it is necessary,

if automatic adjustment is not provided, that the

indentor position be adjusted manually sufficiently

frequently to maintain the above test load

of 750 N ± 20 N.

Run the machine for 80 000 continuous load cycles

and then remove the test piece from the machine

and allow to rest in an unstrained state

for 10,0 min ± 0,5 min.

Remeasure the thickness d2 of the test piece as

specified in ISO 2439 and then carry out the

measurement of hardness index at 40 % ± 1 %

indentation as specified in sub-clause 7.2

(method A) of ISO 2439:1980, including the

preliminary indentation procedure specified in

sub-clause 7.1 of that International Standard,

except that the 40 % ± 1 % indentation level shall

be calculated using the original thickness

measurement d1.

Repeat the whole procedure, from the measurement

of the original thickness and hardness index at the

beginning of this clause, for the two remaining test

pieces.

8 Test report

The test report shall include the following

information:

a) a reference to this International Standard;

b) a description of the material;

c) the conditioning used;

d) the size and shape of the component tested, if

different from the standard test piece;

e) the predominant direction of the cellular

structure, if any;

f) the median percentage thickness loss after

pounding;

g) the median hardness loss after pounding.

NOTE An example of how to express briefly the dynamic

fatigue characteristics determined in accordance with this

International Standard is as follows:

ISO 3385/median percentage thickness loss/median hardness

loss.

4

© BSI 05-1999

EN ISO 3385:1995

Figure 1 — Diagrammatic arrangement for manually adjusted machine

© BSI 05-1999

5

EN ISO 3385:1995

Figure 2 — Diagrammatic arrangement for automatically adjusted machine

6

© BSI 05-1999

BS EN ISO 3385:1995

List of references

See national foreword.

© BSI 05-1999

BS EN ISO

3385:1995

BSI — British Standards Institution

BSI is the independent national body responsible for preparing

British Standards. It presents the UK view on standards in Europe and at the

international level. It is incorporated by Royal Charter.

Revisions

British Standards are updated by amendment or revision. Users of

British Standards should make sure that they possess the latest amendments or

editions.

It is the constant aim of BSI to improve the quality of our products and services.

We would be grateful if anyone finding an inaccuracy or ambiguity while using

this British Standard would inform the Secretary of the technical committee

responsible, the identity of which can be found on the inside front cover.

Tel: 020 8996 9000. Fax: 020 8996 7400.

BSI offers members an individual updating service called PLUS which ensures

that subscribers automatically receive the latest editions of standards.

Buying standards

Orders for all BSI, international and foreign standards publications should be

addressed to Customer Services. Tel: 020 8996 9001. Fax: 020 8996 7001.

In response to orders for international standards, it is BSI policy to supply the

BSI implementation of those that have been published as British Standards,

unless otherwise requested.

Information on standards

BSI provides a wide range of information on national, European and

international standards through its Library and its Technical Help to Exporters

Service. Various BSI electronic information services are also available which give

details on all its products and services. Contact the Information Centre.

Tel: 020 8996 7111. Fax: 020 8996 7048.

Subscribing members of BSI are kept up to date with standards developments

and receive substantial discounts on the purchase price of standards. For details

of these and other benefits contact Membership Administration.

Tel: 020 8996 7002. Fax: 020 8996 7001.

Copyright

Copyright subsists in all BSI publications. BSI also holds the copyright, in the

UK, of the publications of the international standardization bodies. Except as

permitted under the Copyright, Designs and Patents Act 1988 no extract may be

reproduced, stored in a retrieval system or transmitted in any form or by any

means – electronic, photocopying, recording or otherwise – without prior written

permission from BSI.

This does not preclude the free use, in the course of implementing the standard,

of necessary details such as symbols, and size, type or grade designations. If these

details are to be used for any other purpose than implementation then the prior

written permission of BSI must be obtained.

If permission is granted, the terms may include royalty payments or a licensing

agreement. Details and advice can be obtained from the Copyright Manager.

Tel: 020 8996 7070.

BSI

389 Chiswick High Road

London

W4 4AL